## Slide 1: PHY377/477 Soft Condensed Matter
Dr Martin Grell
Slides developed from Prof Mark Geoghegan’s prior material
Based on R A L Jones “Soft Condensed Matter” (OUP, Oxford, 2002)

## Slide 2: Lecture #0 Soft Matter course content
0. Welcome / Introduction
1. Introduction, molecular forces, bulk mechanics
2. Polymers
3. Miscibility(混溶) and Separation
4. Crystallinity（结晶度） in soft matter
5. Chirality（手性） and Liquid Crystallinity（液晶性）
6. Interfaces and Self-assembly（自组装）

## Slide 3
PHY377/477 ‘Soft Condensed Matter’
0. Welcome and general information – Autumn semester 2017/18
Module leader: Dr Martin Grell, m.grell@sheffield.ac.uk, Hicks D30
‘Parallel’ modules: PHY377 / PHY477
Same lectures and exam for 3rd/4th Yr, small difference in other assessment
Lectures: Tue 11am, Thu 9am, for both 377/477
 Sign In!
Supported by MOLE

## Slide 4
Assessment:
PHY377: 80% exam, 20% assessed Homework
PHY477: 65% exam, 20% assessed Homework, 15% Essay
Pass mark: 40% for 377, 50% for 477
Homework: Released Mon 29 Oct on MOLE
Deadline Mon 26 Nov
Submission to Hicks drop box with bar- coded cover sheet
Essay: 477 only Essay topics and detailed instructions
on MOLE now. Submission to Turnitin embedded
into MOLE. Deadline Mon 12 Nov
Exam: More nearer the time
Recommended reading:
Slides, Lecture Notes, and parallel problems on MOLE
RAL Jones, ‘Soft Condensed Matter’, OUP
on Polymers: Polymers: Chemistry and Physics of Modern Materials,
Third Edition J.M.G. Cowie, Valeria Arrighi

## Slide 5
3rd Yr vs. 2nd Yr: No more problems classes / tutorials
!? So how to study / practice / revise?
 Lectures! (not just the first few), incl. Problems Sessions
 Homework = Mini Exam
 Make time for guided self- study
10 credit module: ~ 100 hrs of work vs. 22 lecture slots
 Revision lectures in January
 ‘Parallel Problems’ section on MOLE:
Numbered problems in parallel to lecture, e.g.
…
C1, C2 near- universal: C1 = 17.4 and C2 = 51.6 K = TG – TVF
aT : Williams- Landel- Ferry (WLF) scaling factor
aka ‘time- temperature superposition’ P4.2
…

## Slide 6: Objectives
Appreciate alternatives to conventional solid state physics
‘Molecular materials’, in particular polymers
See physics beyond the periodic crystal
e.g. glasses, ‘scaling laws’, liquid crystals, micelles,..
Meet molecular engineering materials, and devices
e.g. polymers, rubbers, liquid crystal displays
See synergies of Physics with other sciences
e.g. physical chemistry, life sciences
Understand ‘self assembly’ of molecular materials

## Slide 7: Lecture #1 Soft matter aka ‘molecular materials’
What do we mean by ‘soft matter’? ‘Hard’ vs ‘Soft’
‘Molecular materials’
Pt. 1 Introduction, molecular forces, bulk mechanics

## Slide 8: ‘hard’ vs. ‘soft’ matter
Solid state physics: The unit cell is the basic unit
 Periodic crystal, wave- like excitations, E(k)
Often, high melting temperature
But: when dissolved (e.g. water, acid):
Unit cell falls apart. Same chemical elements, but very different properties.
Soft matter: The molecule is the basic unit
 ! Also may form crystals (‘molecular crystals’)
But molecular properties dominate
Localised excitations
Dissolves (e.g. water, organic solvent): Molecules are retained / stay together
Many properties are retained.
Key player: Solvents (incl. water)

## Slide 9: Molecular materials: Carbon ’organic’ molecules: Contains at least one C-H bond
‘Tetraeder’ P1.1
Angle btwn bonds = 109.5o
‘Promotion’
‘Hybridization（杂化）’
C orbitals: 6 e-
1 x 2s + 3 x 2p:
Hybridisation:
4 x sp3 hybrid
4 x sp3 hybrids:
4 x 1 e- orbitals
Want 2nd e-…
4 bonds from sp3 hybrids: ‘Saturated’ C (single bonds only)
Also: sp2, sp hybrids  ‘unsaturated’ C (double/triple bonds)
Different geometry molecular shape
J H van ‘t Hoff
Nobel Prize 1901

## Slide 10: Molecular materials Illustrating（说明） organic molecules and their shapes
e.g. (linear) Hexane（己烷）: 6 saturated（饱和的） (sp3 carbons) + ‘enough’ H
Highly stylised
C and H implied
Note ’zig zag’
from sp3 angle
Acetone（丙酮）: Only ‘heteroatom’ shown
Here, oxygen (O)
Note, double bond: unsaturated middle C
=
Trans-2- butene vs. cis-2-butene: ‘Isomerism’（异构）
Butene（丁烯）:
C=C double bond
Unsaturated (sp2 hybrid)
Butyne（丁炔）:
Triple bond (sp hybrid)
≠

## Slide 11: Molecular materials Examples of organic molecules: Rings
Benzene（苯）
6 sp2 hybridised C in a (planar) ring:
3 Alternate 3 double / 3 single bonds- but where?
Unhybridised p electrons delocalise around ring
‘conjugation’, p electrons
Cyclohexane（环己）
6 sp3 hybridised C in a ring:
saturated, no conjugation
Not planar
Heterocycles（杂环）: Rings with ‘hetero’ atoms (other than C)
Thiophene Furane Pyrrole

## Slide 12: Molecular materials Big rings: Macrocycles
Heme B
Chlorophyll
Valinomycin
Crown ether
18-crown-6
Charles J Pedersen
Nobel Prize 1987
Soft matter device technology:
Photosynthesis, oxygen transport,
ion selection

## Slide 13: Molecular materials Amino acids
Amine
(carboxylic)
acid
Amine + carboxylic acid
 Peptide bond

## Slide 14: Molecular materials Some more organic molecules…
+ one all- important
inorganic molecule…

P1.2
Polystyrene
Polythiophene
Glucose
5-Cyanobiphenyl
An illegal amine
An ionic liquid
(molten organic salt)

## Slide 15: Summary Lecture #1 Soft matter aka ‘molecular materials’
Soft Matter Physics: Physics of molecular materials. Molecules rule over unit cells
Strong chemical bonds within molecules, weaker forces btwn molecules
Mostly: Organic molecules built from hybridised C orbitals + H,O,N,S,P, and ‘water’
A rich ‘zoo’ of molecules
Molecular ‘device technology’, often in wet medium  Life

## Slide 16: Lecture #2 Gases, Liquids, Solids
States of Matter
Forces / energies within / between molecules
Phase diagram, coexistence

## Slide 17: Gases, liquids, and solids
A reminder...
Internal energy of gases is largely kinetic: rotational, vibrational, and translational
Energy of interaction between liquid molecules is comparable to their kinetic energy
The kinetic energy of molecules or atoms in solids is not enough to overcome their energy of interaction

## Slide 18: Potential energy-separation curves
Hard sphere model
Real systems
Force: Strong repulsion at short distance
Weak attraction at large distance, fading to zero for d  infinity
Energy: Minimum -eB at equilibrium distance, a: ‘Bond energy/length’
Applies to both bonds w/in molecules, and interactions btwn molecules
Btwn molecules: eB related to DHvap or ‘cohesive energy density（内聚能密度）’

## Slide 19: Bonding vs. attractive interactions
    Bonds within molecule / crystal
Ionic bonding (Salts)
  Transfer of electrons
  Strong, ~ 6 eV (e.g NaCl,
  weaker in ‘ionic liquids’)
Covalent bonding: Molecules
  Shared electrons / overlapping orbitals
  Strong and directional, (2 ...6) eV
  e.g. sp3 hybridised C-H in organic molecules
Metallic bonding
  Delocalized electrons
    Strong, similar to covalent but undirected. E.g. transition metals, also alloys
Attraction between molecules
van der Waals force
  Incl. dipolar interactions
    U ~ a2r-6 typically ~ 60 meV, comparable to thermal energy ~ 25 meV
Hydrogen bonding
  Hydrogen (H bond donor) interacts with electronegative atoms (H bond acceptor)
  Directional strong(ish), 120…370 meV
Hydrophobic interaction
  Entropic interaction in water ~ 60 meV P2.1
1 eV = 96.5 kJ/mol

## Slide 20: The three (common) states of matter
Temperature
Pressure
Gas
Temperature
Density
Solid
Gas
Liquid
Triple point
Critical point
Coexistence
Liq.
Solid
Crossed area: No single phase
Coexistence
Coexistence occurs even in a pure material
Coexistence is very common in mixtures
(Liquid/solid, 2 liquid phases, …)

## Slide 21: Blends Coexistence of phases is common
‘Binary phase diagram’
Note the axis:
T vs. composition, no p
Blue, yellow::Coexistence
btwn liquid and solid
Melting/freezing, latent heat,
spread over T range
Water / Ethylene Glycol: ‘Antifreeze’（防冻液） (simplified)
‘Eutectic（共晶）’: TE below either melting point due to entropy of mixing
Blend remains liquid to much lower T than either pure material

## Slide 22: Summary: Lecture #2 Gases, Liquids, Solids
3 common states of matter (more to come)
Strong chemical bonds hold molecules together, weaker intermolecular forces make molecules condense
Condensed phases: Solid or liquid
Different phases may coexist even for pure substances
Coexisting phases common in mixtures/blends
Blending favours liquid phase, extending to lower T
‘Eutectic’
Some material contained within this lecture can be found in SCM chapter 2 up to 2.2

## Slide 23: Lecture #3 Mechanical properties of soft matter
Linear mechanical behaviour: Solid vs. liquid
Shear thickening / thinning（剪切增稠/变稀）
Viscoelastic behaviour（粘弹性）
Simple vs complex fluids
Relaxation time and cooperativity（协同）

## Slide 24: Linear mechanical behaviour I

z
F
Dl
A
Hookean (elastic) solid
  Shear stress in response to shear strain (or vice versa)
    Shear stress,  = F/A
    Shear strain, e or  = l/z = tanq ≈ q
  Constant of proportionality is the shear modulus G
    G = /  s = Ge
! Shear strain / modulus (G) vs. tensile strain / modulus (E)
Macroscopic E can be equated to bond energy density, eB/a3 P 3.1

## Slide 25: Linear mechanical behaviour II
Newtonian liquid
  Flow gradient in response to shear strain
    Stress,  = F/A (again)
    Flow gradient (strain rate)
  Constant of proportionality is the viscosity h
    Given by

y
F, v
A

## Slide 26: Shear thinning and thickening
∂/∂t


∂/∂t
∂/∂t


∂/∂t
∂/∂t


∂/∂t
Newtonian fluid
Shear thinning
Shear thickening
Notes: Shear thickening is a dilatant – silly putty is an example.
Shear thinning is exemplified by paints and ketchup. Avoid using thixotropic. It is not strictly correct.

## Slide 27: Viscoelastic behaviour
Not all materials behave as Newtonian liquids or Hookean solids
  Many materials exhibit a time-dependent response to stress
    This is known as viscoelastic behaviour
    Initial response is elastic
    Long time response is viscous
Examples of viscoelastic materials include:
  Molten polymers（熔融聚合物）
  Colloidal systems（胶体系统） (e.g. paint, wet cement, shampoos)

## Slide 28: Relaxation time t
Strain e
Short time: Elastic, modulus G0
Long time: Viscous flow（粘性流动）, viscosity h
Transition at characteristic t
Relaxation time t = h / G0
Typically, t = t(T)
because h = h(T),
G0 often not so much
Reality: Often much smoother
transition
Rough guide: t > 10 s: Solid, t < 10s : Liquid
(RAL Jones, SCM, Fig. 2.5)

## Slide 29: Viscous flow of simple fluids, e.g. water
  Will ‘relax’ by jumping into nearby void
  Relaxation time  = pexp(e/kBT) ‘Arrhenius’
  (Note ‘Boltzmann factor’: Thermally activated overcoming of energy barrier)
    Activation energy ee ≈ 0.4 DH
    (p)-1 ≈ optical phonon frequency of
    corresponding solid (Eyring)
    Typically, p ≈ picoseconds（皮秒）  Short t
     ∞ for T  0 (but freezes long before)
    Many liquids crystallise before t > 10 s (but not all)
SCM Fig. 2.8
Viscous, not elastic, due to short relaxation times
Assume a molecule is temporarily in a higher energy position due to shear.

## Slide 30
Flow of complex fluids: ‘Cooperativity’
Complex fluid: z > 1 molecules to make
way for one to move: ‘Cooperativity’
ee  zee, z increases as T drops
Arrhenius no longer applies
Steeper rise of t with dropping T
Complex fluids reach t = 10s
before crystallising
( h ≈ 1013 Poise（平衡） with typical G0)
Also: t  ∞ at T > 0
SCM Fig 2.13
> 10s : Non- crystalline (‘amorphous’)（非晶） solid, aka ‘Glass’
T(t = 10s): Glass temperature TG
Glass: Mechanically solid, but structured like a liquid (no unit cell)

## Slide 31: Summary: Lecture #3 Mechanical properties of soft matter
Simplistic ‘extremes’ of mechanical behaviour:
 Hookean / Elastic: s = Ge (solid)
 Newtonian / viscous: (liquid)
Soft matter: Often nonlinear and ‘mixed’ properties
Shear thinning / shear thickening
‘Viscoelasticity’: Elastic up to t / viscous at t > t
Temperature- dependent ‘relaxation time’ t(T) = h/G
Different t(T) / h(T) for simple / complex fluids
Simple: Arrhenius, t  ∞ for T  0, Complex: ‘super’ Arrhenius (cooperativity), t  ∞ for T > 0
t > 10s w/out crystallisation: Glass transition
The material contained within this lecture can be found in SCM chapter 2.3

## Slide 32: Lecture #4: The Glass transition
The glass transition: Flow seizing up
  Mechanics:
    ‘strong’ vs. ‘fragile’ glasses
    Vogel- Fulcher, Williams- Landel- Ferry
  Thermodynamics
    Glass transition vs. phase transition
    Kauzmann paradox

## Slide 33: Glasses are common
Polymers (most interesting here), also some solvents ( e.g. toluene)
Oxide glasses, e.g. (Si/Na/Ca) oxides (windows)
Chalcogenide glasses, e.g. GeS (low gap semiconductors)
Some Elements (S, P, Se)
Magnetic metals when rapidly cooled (‘spin glasses’)

## Slide 34
Recap: ‘Cooperativity’ in complex fluids
Complex fluid: z > 1 molecules to make
way for one to move: ‘Cooperativity’
eB  zeB, z increases as T drops
Arrhenius no longer applies
Steeper rise of t with dropping T
Complex fluids reach t = 10s
before crystallising
( h ≈ 1013 Poise with typical G0)
Also: t  ∞ at T > 0
SCM Fig 2.13
> 10s : Non- crystalline (‘amorphous’) solid, aka ‘Glass’
T(t = 10s): Glass temperature TG
Glass: Mechanically solid, but structured like a liquid (no unit cell)

## Slide 35
‘Strong’ glasses:
Arrhenius behaviour h ~ t
h  ∞ for T  0
All polymers, and many others:
‘fragile’ glasses:
Vogel- Fulcher (VF)
 ∞ for T  TVF > 0
TVF ≈ TG – 50K
Tg Mechanics: h(T) at glass transition
No ‘glass blowing’ with fragile glasses

## Slide 36
Polymer glasses: WLF
  Fragile glass viscosity h vs. T scales with VF
  Relaxation time t ~ h, apply VF for t(T), referenced to tG P4.1
C1, C2 near- universal: C1 = 17.4 and C2 = 51.6 K = TG – TVF
aT : Williams- Landel- Ferry (WLF) scaling factor
aka ‘time- temperature superposition’ P4.2
Logically equivalent to VF, again divergence aT  ∞ ~ 50K below Tg
Engineering: Material mouldable（可塑） at high T / keep shape at ambient（周围） T: ‘Thermoplastics’ (‘Plastics’ for short)
t(T) / tG :
Relaxation times at T / at TG

## Slide 37: TG vs. Phase transitions
First order PT
  Discontinuity in (∂G/∂p)T = V
  Discontinuity in (∂G/∂T)p = S
  ‘1st derivatives of G’
  (Gibbs enthalpy)
Second order PT
  Discontinuity in (∂V/∂T)p = bV
  Discontinuity in −(∂V/∂p)T = kV
  Discontinuity in (∂S/∂T)p = cp/T
  ‘2nd derivatives of G’
Both 1st/2nd order PT: Equilibrium  (different) equilibrium
Glass transition: (non)- equilibrium  non- equilibrium: Not a PT
Glass transition:
(different) discontinuity in 2nd deriv’s.
(Step not divergence)
Heat capacitance vs. T for a polymer
going through TG. Measured by ‘DSC’
Notes: dG = -SdT + Vdp for a reversible path

## Slide 38: TG: Thermodynamics
The glass transition is not a thermodynamic (phase) transition
  It is a kinetic transition
  TG somewhat rate dependent
  - But there’s a limit…
Volume or Entropy
Temperature
Tm
Tg1
Tg2
Volume expansivity changes discontinuously: cooling rate for Tg1 is less than that for Tg2
S calculated by integrating heat capacity cp
  cp = T(∂S/∂T)p

## Slide 39: Entropy and TG: Kauzmann paradox
Entropy
Temperature
Tm
Tg1
Tg2
TK
 Note: TK ≈ TVF, where t, h  ∞
Paradox avoided thanks to t  ∞: Even ‘infinitesimally’ slow cooling cannot keep S(T) on ‘supercooled liquid’ line.
Glass below TVF = permanent non- equilibrium. Usual thermodynamics suspended
 No (thermodynamic) Maxwell relations, no Clausius Clapeyron, no eutectic for TG in blends. Also, S > 0 for T  0  3rd law
Extrapolate supercooled liquid （外推过冷液体）S(T)
below TM to TK:
S(liq) would drop below S(Xtal)
Paradox !?
TK: Kauzmann temperature
From extrapolation: TK ≈ Tg – 50K

## Slide 40: Summary: Lecture #4 The Glass transition
Complex fluid: Vogel Fulcher h(T) due to cooperativity
Steeper rise of h as T drops, often reaches t = 10s before crystallising: Glass transition
VF h  WLF: ‘Time- temperature- superposition’
t  ∞ at TVF ≈ TG - 50K. Near- universal constants C1, C2
Glass mechanics: Non- crystalline solid
- Glass thermodynamics: Equilibrium  non- equilibrium
not a phase transition
Kauzmann ‘paradox’ at TK ≈ TG – 50K
but t  ∞ avoids paradox
For a given material, TK ≈ TVF ≈ TG - 50K
Something interesting is going on
The material contained within lecture 4 is covered in SCM chapter 2.4