## Slide 1: Pt. 6 Interfaces and Self Assembly Lecture #18 Interfaces and amphiphiles
Self-assembly of soft matter:
Interface tension
Hydrophophilic vs. Hydrophobic
Amphiphiles and surfactants
Self Assembly in water: Micelles / microphase separation
Micelle geometry
Critical micelle concentration (CMC)
H
H
H
H
H
H
H
H
O
O
O
O

## Slide 2: Interfaces between phases Liq/Liq phase separation (Ch. 3) implies interfaces Macroscopic:
Immiscible liquids: Interface is unfavourable, but moving wire by distance Dx creates more- hence, work DW to do
(Usually isothermal, so strictly, work is a H’holtz Free energy)
 Force F on wire, F = DW/Dx
 F ~ L, define interface tension g
F = 2L  g = F/2L = DW/2LDx
Unit of g: N/m or J/m2
is a property of the 2 liquids in contact
g = g(T)
Notes: Be clear about what the factor of 2 is for. This is the capillary wetting of the wire, and you are essentially pulling the wire distance x out of the fluid. Obviously if x is too large the wire comes out of the fluid, but for small x this is not a big problem because you just create more fluid interface.

## Slide 3: Molecular- level model of interface energy Back to the lattice model
Assume ‘sharp’ interface
Calculate interface energy DW per cell in lattice model P18.1
Assume cell = cube of side a, a = V01/3, V0: Volume of 1 molecule
LDx = a2 for one cell
Real g < gsharp,
interfaces are ‘blurred’
by Brownian motion
Sharp
interface
Interface tension is discussed
in SCM 3.2.1

## Slide 4: Flashback We already used interface tension = surface energy
Homogeneous crystal Nucleation
describes melt/crystallite surface energy
DG = 2a2sf - La2DHmDT/Tm(∞)
Polymer Xtal Lamellae
sf describes fold surface energy
Heterogeneous
nucleation

## Slide 5: Hydrophilic vs. Hydrophobic surfaces
‘Hydrophilic’ surface:
Good wetting with water
Small gSL, small ‘contact angle’
e.g. solid oxides
‘Hydrophobic’ surface:
Poor wetting with water
Large gSL, large ‘contact angle’
e.g. waxed surface
Contact angle given by interface tensions g (Solid/Liquid/Gas)
Young eqn.:
Reason @ molecular level:
H- bonding (h’philic) vs.
Hydrophobic interaction (odd)

## Slide 6: Amphiphiles
Molecules which have hydrophobic and hydrophilic parts
  Polar or ionic hydrophilic ‘head’ (Anionic, cationic, or non-ionic)
  Chemically bonded to hydrophobic alkyl chain ‘tail’
Sodium stearat: Soap (anionic)
Sodium dodecyl
sulfonate (SDS):
Laundry powder
(anionic)
Dodecyl glucoside:
Shampoo (non- ionic)
Notes: Worth asking about surfactants - not just in detergents, but also in the extracellular matrix etc. octanol and SDS shown here. Note octanol is not miscible in water, but methanol is. It is worth discussing the effect of the alkyl chain in miscibility with water. 1-propanol is pretty miscible with water, but n-butanol is only partially miscible with two phases; one containing 32% w/w water and the other (less dense) containing 5% w/w n-butanol.

## Slide 7: Amphiphile as detergent
Amphiphile accumulates at oil/water interface:
Hydrophobic end in oil, hydrophilic head facing water
 Reduced interface energy/surface tension
 Allows formation of more surface
 stable ‘Emulsion’ of small oil droplets
3- component mix: Water / ‘oil’ (hydrophobic liquid) / amphiphile

## Slide 8: Amphiphile as surfactant
Low conc.: Amphiphile dissolves, some accumulate
at surface  Graded water/air transition,
reduced surface tension
Increasing conc.: Surface tension decreases
‘Excess’ conc.: Amphiphile ‘saturates’
forms ‘droplets’ w/out oil:
‘Micelles’, ‘microphase separation’: Equilibrium
above ‘critical micelle concentration’ (CMC)
2- component mix: Water / amphiphile ‘surfactant’
(Wikipedia)
G Pourceau et al,
Molecules 2016, 21(10), 1301

## Slide 9: Critical micelle concentration (CMC)
As you add amphiphile to water, first it all dissolves/goes to surface.
Micelles only appear above CMC.
Above CMC, all additional amphiphile then goes into micelles
Similar to liquid/liquid phase separation:
Small fraction F << 1 of ’immiscible’ liquid does dissolve / mix
e.g. SDS, 20 oC:
CMC c = 8.2 mM
(note c vs. F) P18.2
CMC = CMC(T)
Minimum T needed
for some amphiphiles
(‘Krafft Temperature’)

## Slide 10: (Spherical) Micelles: Optimum N = M
EN (energy/molecule) has a minimum at N = M
Micelle size M favoured over both
- isolated molecules (N = 1, solution)
- ‘macro’ phase separation (N  ∞)
(e.g. water/oil)
e.g. SDS: M = 62
Different for cylindrical micelles
- ‘infinitely’ long gives lowest EN

## Slide 11: CMC for spherical micelles - a simple theory -
XN: Volume fraction of molecules in N- size micelles (isolated / dissolved molecule: N = 1)
Total vol. fraction
Equilibrium condition: Chemical potential equal across all micelles

## Slide 12: CMC for spherical micelles - a simple theory -
Assume only two fractions: Isolated/dissolved amphiphile (N=1), X1,
or amphiphile in optimum sized (M) micelle, XM
(Fair for spherical, not for cylindrical)
 P18.3
If X1 < exp(-DE/kBT): XM << X1, almost all molecules are dissolved,
Amphiphile volume fraction F ≈ X1
Critical micelle concentration (CMC) X1 = Fc = exp(-DE/kBT)
(Note the misnomer- Fc is a volume fraction, not a concentration!)

## Slide 13: Different micelle shapes: Not just spheres
Bilayers
Cylindrical (Wormlike) Micelles
Spherical Micelles
Hydrophobic-Hydrophilic molecule
Slide courtesy of M R Tomlinson

## Slide 14: Cylindrical/spherical micelles? Bilayers?
lc
a0
Amphiphile geometry:
Maximum/stretched length of alkyl chain, lc
Area of head group a0
Hydrophobic (hydrocarbon) volume v (shaded)
Note: a0 is not purely geometric for charged head group
v
Define ‘Micelle packing parameter’
p = v/a0lc (dimensionless)
Small p  spheres
Medium p  cylinders
Large p  Bilayers

## Slide 15: Quantitative micelle geometry
Sphere of M molecules: Mv = V = 4r3/3; Ma0= A = 4r2
Ratio V/A = v/a0 = r/3 < lc/3  v/a0lc = p < 1/3
Cylinder of M molecules: V = pr2l = Mv; A = 2prl = Ma0
Ratio V/A = v/a0 = r/2 < lc/2  v/a0lc = p < ½
p < 1/3 : Spherical micelles; 1/3 < p < ½: Cylindrical micelles
p > ½: Bilayers
Bilayers: E.g. Phospholipids
2 h’phobic tails per h’philic head
Large v  Bilayers
Biological membranes
Microphase separation
 ‘Self assembly’

## Slide 16: Summary: Lecture #18 Interfaces and amphiphiles
Interfaces btwn immiscible liquids cost energy, quantified by g
Important example: Water/solid interfaces, ‘hydrophilic’ vs ‘hydrophobic’
Amphiphiles are molecules with hydrophobic and hydrophilic units, act as detergents and surfactants
Amphiphiles in water can micro- phase separate into micelles
Critical Micelle Concentration (CMC)
Spherical/cylindrical/bilayer micelles
Amphiphile geometry (p)
The material contained within this lecture can be found in SCM Ch. 3.2, and Ch. 9 from 9.1 to 9.2.2

## Slide 17: Lecture #19 Block copolymer self assembly
Another micro- phase separation
e.g. PS-b-PMMA diblock copolymer
PS and PMMA are incompatible
 Phase separation
But can’t macro- phase separate
Because the blocks are chemically bonded
Both atactic  don’t Xtallise

## Slide 18: (Di)Block copolymers
Block copolymers form varied morphologies
  Require immiscible blocks,  > 2/N
  Morphology depends on the ratio f, f = n / (n + m)
  Simplest: Lamellar (L)
  similar block sizes (f ≈ ½)
  (Do not confuse with Xtal lamellae!)
  Another micro- phase separation
  Leads to regular large- scale structures
  Without crystallinity
from SCM

## Slide 19: Diblock copolymer morphologies Phase diagram
N = n+m: Total No. of repeat units in chain
f = n/N: ratio of block lengths (f = ½ means n = m = N/2)
W van Zoelen, G ten Brinke, Soft Matter 5, 1568 (2009)

## Slide 20: Lamellar morphology
Here the two blocks are of similar size, n ≈ m (f ≈ ½)
Phase separation even for small positive c
‘Lamellae’ – but amorphous - not to be confused with crystalline lamellae
Scaling of lamella thickness d with N? d ~ Nb (Note: N ≈ 2n, so same scaling)
d

## Slide 21: Block copolymer lamellae: d = ?
Lamella interfaces are unfavourable
  The interfacial free energy per chain is
    The interfacial energy per unit volume scales as g /d
    There are 1/(Na3) chains in unit volume
Fint minimised by large d  stretch chains
But stretching reduces entropy, gives rubber- elastic energy
Minimise the total free energy, F = Fel + Fint , w.r.t. d P19.1
  Scaling law for lamella thickness: d ~ N2/3
  Surface tension g stretches coils. Compare to R ~ N1/2 in homopolymer melt; R ~ N3/5 in good solvent

## Slide 22: SBS (‘Kraton’) synthetic rubber
Poly (styrene-butadiene-styrene) (SBS) triblock copolymer
(TEM, Styrene blocks light)
Hexagonal nanostructure
Polystyrene blocks: Tg ≈ 100 oC
Polybutadiene blocks: Tg ≈ -90 oC
At ~ 170 oC: Process from viscous
melt (thermoplastic).
At ambient: Polybutadiene
‘physically crosslinked’
Rubber aka Elastomer
‘Thermoplastic elastomer’
Physics + Chemistry

## Slide 23: Summary: Lecture #19 Block copolymer self assembly
Variety of regular structures through microphase separation
Phase diagram for diblock copolymer structures
Lamellae: Minimising interfaces stretches block coils, d ~ N2/3
Microphase separated SBS: Thermoplastic elastomer
The material contained within this lecture can be found in SCM 9.3.2

## Slide 24: Recurring themes summary
Scaling laws: A polymer size proportional to number of repeat units to a power
Globule (collapsed coil), R ~ N1/3; Melt/Q solvent: R ~ N1/2;
Good solvent: R ~ N3/5; Block copolymer lamellae: d ~ N2/3
Mean field theories: Approximate treatment of statistical physics problems
Self- avoiding random walk (SARW) R scaling, lattice theory of liquid/liquid mixing or phase separation, nematic LC ordering
Microphase separation / self assembly: Parts of molecules try separate from each other, but are tied together by chemical bonds
Smectic A LC, amphiphile micelles, block copolymers