## Slide 1: Pt.3 Miscibility（混溶性） and Separation Lecture #9 Lattice theory: The ‘regular solution’ model The fudge factor lecture
Introduction to phase transitions
Basic thermodynamics
Simple mean-field theory of liquid/liquid mixing / phase separation

## Slide 2: What causes a phase transition?
Equilibrium at global minimum of thermodynamic potential
Usually Gibbs (G) or Helmholtz (F or A) free energy P9.1
Local minima depend e.g. on T
As T changes, one local minimum can undercut（咬边） another
 different equilibrium state at high vs. low T
Phase transition at Ttr where local minima equal
Coexistence of 2 phases at Ttr even for single substance
Coexistence over wide T range possible in mixtures
Notes: G = U + PV -TS = H - TS: also need to mention chemical potential
F = U - TS

## Slide 3: Equilibria aren’ t everything…
Equilibrium not always reached
  Energy barriers may interfere
    Metastable state
  Glass transition may arrest development
    Also allows interesting structures to be ‘frozen’ in
Notes: Here dG = dU +pdV + Vdp - TdS - SdT is worth introducing, because then we can use dQ = dU + pdV and dQ = TdS to simplify things.

## Slide 4: Will 2 liquids mix? PT within liquid state- no solidification or boiling
Btw: Similar for polymer solubility
But ‘black’ component linked into
N- chain  later
‘Lattice theory’
Mentally divide
space into cells
Each cell accommodates one molecule of either liquid, just enough cells for all molecules
z nearest neighbours
xA (moles) liquid A
xB (moles) liquid B
Volume fractions
FA/B = xA/B / (xA + xB)
FA = F; FB = 1-F
Note symmetry A vs. B
Don’t be fooled by appearances,
we are talking about liquids,
the lattice is just a counting aide
NOT a Xtal lattice.
Assume number fraction
= Volume fraction
Concentration measured
as volume fraction
Ignore ‘excess volume’
V = const.  F = U - TS

## Slide 5: Entropy of mixing Smix= DS DS = Smixed - Sseparated
More convenient to work in volume fractions FA, FB
FA = F,
FB = 1 - FA :
note, symmetry btwn A/B is retained (as symmetry btwn F / 1-F)
Mixing decreases F = U – TS  Entropy always favours mixing
(unless we have hydrophobic interaction)
‘Counting’ permutations（排列）: Separated: xA!xB! vs. mixed: (xA+xB)!
Entropy S ~ ln(permutations); Stirling: ln(M!) ≈ MlnM
P9.2

## Slide 6: Energy of mixing, Umix = DU DU = Umixed - Useparated
Each molecule has an energy of interaction with its neighbours on the lattice
  Like-like interactions: AA or BB
  Like-unlike interactions: AB = BA
Notes: At this point, one should introduce the lattice arguments provided by Rubinstein and Colby (and Jones in SCM). It is interesting to note that the simple lattice arguments agree with arguments based largely around perfect gases.

## Slide 7: Pairwise（成对） interactions
Assume interactions with z nearest neighbours, random pairing in mixed state (mean field assumption)
U (mixed)
U (separated)
P9.3

## Slide 8: Energy of mixing, Umix = DU DU = U(mixed) – U(separated)
When A/B interact by vd Waals only: c > 0 P9.4
DU often positive  favours separation
Define ‘interaction parameter’ c
dimensionless
=

## Slide 9: (Helmholtz) free energy of mixing
F = U –TS  Fmix = DF = DU - TDS
(FA = F, FB = 1-FA = 1-F)
Mean- field expression for liquid/liquid DF
Note the symmetry btwn A/B, or F / (1-F). Fails reality check…
Simple lattice theory: c = c(T) = A/T  Reality: c = c(T,F)
 c is used as ‘fudge factor’
+

## Slide 10: Summary: Lecture #9 Lattice theory
Simple lattice- based reasoning allows calculation of entropy and energy of mixing
Entropy always favours mixing (except h’phobic entropy), energy usually favours separation
Enter the interaction parameter c for DU
Energy/entropy combined into simple eqn. for F of mixing
Lattice model cuts corners e.g. DV, hydrophobic interaction
Use c as ‘fudge factor’
The material contained within this lecture can be found in SCM chapter 3 up to 3.2

## Slide 11: Lecture #10 Mixing and separation
Phase diagrams from DF / kBT
Types of phase separation

## Slide 12: Plotting DF(F,c)
from SCM
T dependency
Implied in c
Note symmetry
w.r.t. F / 1-F
ccr = 2
F
+

## Slide 13: Stability, instability, metastability, coexistence
from SCM
In the right hand diagram, 1 and 2 are known as co-existing compositions.
Not pure substance A/B! 1/2 ≠ A/B!
Unstable, not even locally stable
Globally unstable,
but locally stable ‘metastable’
DF(F) convex:
Stable mix
Phase separation
into 2 co- existing
liquid phases
Vol. fraction a @ F1
1 - a at F2
P10.1
Notes: Need to be clear about the difference between volume fractions and the fractional volume covered by each component. One must not mistake volume fraction for 100% of one component covering phi% of the volume. Therefore the factors f need to be introduced.

## Slide 14: Phase diagrams
from SCM
‘Universal’ binary phase diagram
(F/c) plane
Specific phase diagram F/T plane
(c(T) not universal)
‘Upper Critical Solution Temperature’ Tcr
UCST
Note, F symmetry / Fcr = ½ w/in lattice model – but not in reality!
P10.2
Coexistence curve aka ‘binodal’ or ‘cloud point curve’ (stable/metastable): d(DF/kBT)/dF = 0
Spinodal: Metastable/unstable d2(DF/kBT)/dF2 = 0
Critical point:
1st/2nd/3rd derivative DF/kBT to F = 0  ccrit = 2

## Slide 15: Forms of phase separation
Spontaneous (spinodal decomposition)
  Requires no activation energy/nucleation
  Leads to ‘kinetic’ pattern formation: One length scale grows fastest (Cahn Hilliard model, more in SCM 3.3.2 onwards)
  Metastable (binodal decomposition): Nucleation required
Homogeneous nucleation
  Thermal activation required
Heterogeneous nucleation
  Impurities allow one phase to condense, triggering phase separation

## Slide 16: Summary Lecture #10 Mixing and separation
Shape of DF(F) depends on T (via c)
c < 2 (usually, high T): Stable mix for all F
c > 2 (usually, low T): Phase separation for F1 < F < F2. Coexisting vol. fractions F1, F2
W/in lattice model, F2 = 1- F1 - not really though
But always (a = vol. fraction occupied by F1 phase)
Different modes of phase separation
(unstable vs. metastable  spinodal / binodal)
This is in SCM 3.2

## Slide 17: Lecture #11 Polymer solubility and miscibility Another Flory lecture
Extending the lattice model to polymer solutions

## Slide 18: Lattice theory for polymer solutions/blends ’Flory- Huggins theory’
Polymer solution
N: Degree of polymerisation (‘length’)
xA/N (moles) polymer
xB (moles) solvent
Volume fractions
FA/B = xA/B / (xA + xB)
FA + FB = 1
FA = F, FB = 1 - F
Solution:
Blend:
Polymer blend
xA/NA(moles) Polymer A
xB /NB (moles) Polymer B
Volume fractions
FA/B = xA/B / (xA + xB)
FA + FB = 1
=> FA = F, FB = 1 - F
Entropy N- times reduced by ‘chain’ condition
Solution: ccr  ½ for N  ∞ ; Blend: ccr  0 for (NA and NB )  ∞

## Slide 19: ‘Incompatibility’
Polymer solutions:
Entropy of solution significantly reduced
Solvents must be chosen carefully
Rule- of thumb: matching
‘Hildebrand’ parameter d
There are exceptions (e.g. acid/base)
Polymer blends:
Entropy of mixing btwn 2 high N polymers virtually zero
Mixing must be enthalpy (c) driven- but usually isn’t - most polymers phase- separate
Exceptions, e.g. PMMA/PVC
‘Incompatibility’ troublesome for polymer recycling
Incompatible polymers may still share common solvent
Separation may be arrested by Tg
Chemistry wins (block/graft copolymers, e.g. HIPS, ABS)

## Slide 20: Polymer solubility: The Q temperature
- Discuss
Critical point: First /second/third derivative to F = 0
Fcr ≈ N-1/2 (N >> 1)
( Fcr = ½ for liquid/liquid mix: Phase diagram skewed to low F)
 ccr ≈ ½ + N-1/2 (N >> 1)
( ccr = 2 for liq/liq mixtures: Solubility needs smaller c)
Flory defined Q Temperature by c(Q) = ½
½ = Limit of ccr for N  ∞; (Q - Tcr ) ~ N-1/2
< ½ : Good solvent, R ~ N3/5
= ½: Q solvent, R ~ N1/2
> ½: Poor solvent (or non- solvent), R ~ N1/3

## Slide 21: Example Q- Systems / Temperatures
Polymer | Solvent | Q [oC]
Polystyrene (PS) | Cyclohexane | 35
Polystyrene (PS) | Decalin | 27
Poly(a-methylated)styrene | Cyclohexane | 34
Polymethyl methacrylate (PMMA) | 4-Heptanone | 32
Polyacrylic acid | Dioxan | 29
Polymethacrylonitrile | Butanone | 6
Polyethylene (PE) | Nitrobenzene | 230
Polyethylene (PE) | Biphenyl | 125
Polypropylene (PP) | Diphenyl ether | 133
Polyisobutylene | Diisobutylketone | 58
condition is property of Polymer/solvent system
‘Q solvent’ is meaningless without specifying the polymer, and the Q temperature

## Slide 22: ‘Flory Huggins’ interaction parameter c when used for polymer solutions
Often of the form  = -A + B/T
  Sometimes  is included
    Composition dependent  is more complicated
  These are UCST phase diagrams if B > 0
    Upper critical solution temperature
Sometimes we have LCST phase diagrams
  Here different expansivities may be important
  Water as solvent / hydrophobic interaction
Other possibilities
  Both LCST and UCST in the same mixture and “hour glass” forms are possible

## Slide 23: Phase diagrams for c = -A + B/T
Polyisobutylene/Diisobutylketone
Mw up: UCST  Q = 58 oC, Fc  0
Limit N  ∞: Tcr  Q, Fcr  0
(Q - Tcr ) ~ N-1/2
P 11.1
Q
UCST Phase diagrams
Tcr increases as N increases
Fcr decreases as N increases

## Slide 24: c ≠ -A + B/T: Other phase diagrams
PS/acetone
Different
Mol. Wt.
Poly(ethylene oxide)/water
(  M = 5000 g/mol,
x M = 3000 g/mol)
‘Lower critical solution Temperature’
LCST
Hydrophobic (and similar) interactions:
Entropic contributions other than combinatorial S
(Wrongly) accounted for as enthalpies, fudged into c
Both UCST and LCST
(low M Wt)
High M Wt:
Upper Tcr drops below lower Tcr
’Hourglass’

## Slide 25: Summary: Lecture #11 Polymer solubility and miscibility
Lattice model can be adapted to polymer solutions and blends
Entropy of mixing is reduced N- fold
Most polymers are ‘incompatible’, i.e. don’t mix with other polymers
Most polymers still dissolve in well- chosen solvents
Polymer/solvent phase diagrams are skewed to low Fpolymer (i.e. critical point at Fpolymer << ½)
Key concept in polymer solution thermodynamics: Q temperature / solvent / condition
SCM does not deal with polymer solutions as prominently as specific polymer science texts. Cowie and Arrighi dedicate a full chapter to polymer solutions. And H Morawetz, ‘Macromolecules in Solution’, dedicates a whole textbook.