## Slide 1: Pt 4: Crystallinity in soft matter Lecture #12 Crystallisation in soft matter
Getting from melt  crystal in soft condensed matter, and in general
Crystallinity in polymers?

## Slide 2: Crystallisation: Liquid  Solid phase transition Requires nucleation, similar as for binodal phase separation
  At Tm solid and liquid have equal Gibbs potentials
    DHm: Latent heat of melting; Sm = Hm/Tm entropy of melting (Here understood per unit volume, not per mole as usual) P12.1
    Thermodynamics assumes ‘infinite’ crystals, ignores surfaces
    But crystals start out small…
    Nucleation (size r) costs surface energy ~ r2
    Undercooling is necessary for crystallisation

## Slide 3: Nucleation
  Undercooling by DT  Gbulk = -THm/Tm
   Favourable DG ~ r3 (Volume) for nucleus of radius r
But unfavourable interfacial energy ~ r2 (area)
gSL: Solid/liquid interfacial energy
Assuming spherical Xtal- not strictly realistic but Vol. ~ r3 / Surf. ~r2 is
= -
Notes: Since delta Sm = dG(solid)/dT - dG(liquid)/dT = delta Hm/Tm [all at constant pressure]

## Slide 4: Critical radius
Adding surface and bulk terms together shows that small nuclei raise the Gibbs potential
from SCM
Crystal nuclei (‘embryos’) must overcome r*
before they grow spontaneously P12.2

## Slide 5: Nucleation and undercooling
Substitute critical radius into free energy
 Nucleation rate ~ exp(-G*/kBT)
  Strong function of DT: DT  0: Nucleation rate  0:
  Melt never crystallises @ Tm, ‘undercooling’ DT needed
‘Homogeneous nucleation’
Only dominates in very pure liquids
Nucleation increases with DT, but so does h  Crystallisation may be ‘outrun’ by vitrification, i.e. forming a glass- not unusual for molecular materials, particularly common in polymers.

## Slide 6: Heterogeneous nucleation Impurities, or vessel walls
‘Flat cap’ geometry at the wall of a vessel geometry reduces DG*
DG* ~ (1-cosq)2(2+cosq)  0 for q  0
Practically, heterogeneous nucleation usually dominates
‘Ideal’ heterogeneous nucleus:
Seed crystal of same material, > r*
‘Czochralski process’, Si single Xtals
Notes: ΔG* here is simply the previous ΔG* multiplied by V/(4πr3/3)

## Slide 7: Crystallization rate: Growth of nuclei
Avrami equation is primitive description of crystallization kinetics.
  Still commonplace, often used for polymers
cr = 1 - exp(-Ktn)
  K= K(T), t time, and cr crystallized volume fraction (‘degree of crystallinity’)
    Avrami theory: n is an integer, between 1 and 4
      Now n is regarded as a fit parameter, not always integer
But note: For polymers, real cr does not approach 1 for t  ∞
Avrami plot : straight line, slope n
Notes: n = 1, 2, and 3 for each dimension, because the growth of each lamellae is proportional to t. Instantaneous crystallization has an Avrami exponent 3, because nucleation is no longer time dependent. The preceding sentence applies to only early times because it is linear in t. In reality, crystallization depletes the bulk polymer of material to crystallize, so the decaying exponential is more appropriate (and can be mathematically proven). Of course, Avrami behaviour is a bit hand-waving and divorced from reality.

## Slide 8: Crystallinity in polymers ?
Crystals of ‘small’ materials are not usually perfect
- vacancies, interstitials, dislocations, grain boundaries/twinning,...
But: In principle, ‘infinitely’ large in 3 dimensions
Some polymers may crystallise, but…
 Not all polymers can- depends on molecular architecture
 Even in polymers that can- Xtallinity often frustrated by vitrification ‘quenching’
 Polymer crystals are not ‘infinite’ in all 3 dimensions
Always finite in the axis // chain backbone
Flat sheets (‘lamellae’): Surface energies never fade away
 Some non- crystalline regions always remain: ‘Degree of crystallinity’ Fcr < 1
 Permanent non- equilibrium state, incomplete order, hierarchies of structure
OK there’s one exception:
‘Topochemical polymerisation’
e.g. Polydiacetylene
G Wegner Z. Naturforschg. 24b, 824 (1969)

## Slide 9: Polymer structure Xtalisation
(Lack of) tacticity, e.g. PS,
PMMA aka ‘Perspex’
or alternating vs. random copolymers
? highly Xtalline amorphous, TG ~ 100 oC
Branching, e.g. LDPE vs. HDPE
‘Quenched disorder’ impedes Xtallinity

## Slide 10: Summary Lecture #12 Crystallisation in soft matter
Crystallisation needs nucleation
Homogeneous nucleation needs supercooling
no crystallisation at Tm
Often heterogeneous nucleation dominates
Crystallisation kinetics often fitted by Avrami eq.
Some Polymers also can crystallise
Others can’t, depends on ‘quenched disorder’ in chain architecture
Polymer Xtallisation slow, can be ‘quenched’
Polymer Xtals don’t extend  ∞ in all directions
Polymers don’t crystallise fully; Fcr < 1
Some of this is in SCM 3.4.1

## Slide 11: Lecture #13 Polymer crystallisation I
Experimental study of Polymer Crystallinity
- Calorimetry, X-rays, polarisation microscopy
Polymer crystal morphologies
- Lamellae, spherulites, shish kebabs

## Slide 12: Measuring/quantifying polymer crystallinity
 Measures flow of heat as T is ramped
up or down, ≈ (5…10) oC/min
Glass transition: Step up
Crystallisation: Peak down
Area = Heat of fusion
Melting: Peak up
Area = Latent heat of melting
‘DSC’: Differential Scanning Calorimeter
Example DSC scan:
T 
Polymers often Xtallise on heating
Then melt again at higher T

## Slide 13: Measuring/quantifying polymer crystallinity
‘WAXS’: Wide- angle X-ray scattering’
wide angle  small size structures
iPP, 137 oC
Lamella thickness d:
Scherrer equation
(K ≈ 0.9, l: X-ray wavelength)
t = 0: Amorphous ‘halo’
t > 0: Peaks grow as
iPP Xtallises
Sharp- ish Peaks , but
finite width
 finite lamella thickness
Degree of crystallinity Fcr
Typical d ≈ (10… 20) nm
Polymer Journal (2013) 45, 87–93

## Slide 14: Making polymers Xtallise
Macromolecules 32, 5810 (1999)
X- ray fibre diffraction of
aligned poly(fluorene)
Treatments:
a.) fibre rapidly cooled,
aligned but glassy
b.) thermal crystallisation
Anneal @ favourable T
c.) ‘solvent anneal’
Expose to solvent vapour
d.) b+c combined
fibre axis

## Slide 15: Polymer crystals at nanoscale: Chain- folded lamellae
L
Lamellae grow sideways by polymer stems joining from melt.
Lamella thickness L ≈ 10nm << contour length Na, ≠ R, independent of N
At surface, chains fold back into lamella, or join other lamella: ‘tie fibril’
Once L is established it does NOT grow
Surface : Bulk remains finite, does not fade  0
Unfavourable lamella surface energy eats into DG gain from crystallisation
Lamellae lock in permanent non- equilibrium, Tm(L) < Tm(∞)
So…
1.) How can we know Tm(∞)?
2.) What controls L, if not equilibrium?

## Slide 16: Measuring/quantifying (polymer) crystallinity
Polmiscope sees birefringence
iPP ‘spherulites’ ~ 100 mm scale ‘Maltese Cross’
Much larger than typical lamellae … ? …
Watch them grow over seconds/minutes/hrs
(T – dependent rate)
+ hotstage:
B Cheng, JRG Evans, Soft Matter 5, 3572 (2009)
Also, AFM…

## Slide 17: Spherulites: Bundles of lamellae
A spherulite grows by the condensation of chains on them forming more and more lamellae
Image courtesy of Professor A M Donald

## Slide 18: Shish kebabs
Chain-folding occurs in different geometries
  does not require pre-existing crystal face
  ‘Shish’: Crystallised
  aligned (stressed) polymer
  ‘Kebab’: Epitaxial growth
  on shish
A. Keller Faraday Discuss. Chem. Soc. 68 145 (1979)
polyethylene shish kebabs

## Slide 19: How do we know Tm(∞) ?
Crystallise polymer isothermally at Tc, TG < Tc < Tm(∞)
Measure Tm, Tm > Tc: Tc < Tm < Tm(∞)
Repeat for several Tc approaching Tm(∞)
Plot Tm(Tc), extrapolate to Tm = Tc = Tm(∞)
A poly(propylene oxide)
From RL Young,
Introduction to Polymers
P13.1
Tm(∞)
(Or, plot Tm-Tc vs. Tc and extrapolate to zero)
Tm(∞) independent of N / Mol. Wt.
Tabulated in Polymer Handbook

## Slide 20: Summary: Lecture #13
Key experimental techniques: DSC, X-ray, Polmiscope
Polymer Xtals = chain folded lamellae
Finite lamella thickness L, Tm(L) < Tm(∞)
We can find Tm(∞) by extrapolation
Lamellae bundle into spherulites, or as ‘shish- kebaps’
- Hierarchy of structures
Some of the material contained within this lecture can be found in SCM 8.2.

## Slide 21: Lecture #14 Polymer crystallisation II
Kinetic Theory of polymer chain-folded lamellae
  Thermodynamics
  Fastest growing length scale
  Speed of crystallization

## Slide 22: Lamella Thickness L: Growth kinetics
L is a compromise
  Thick lamellae require a high entropic cost to straighten a polymer chain segment
  Thin lamellae have too many fold surfaces
  Either gives slow
  growth rate, n
L(Tc) given by L with fastest n at given Tc < Tm(∞)
Straightening chain so it can join as a stem costs entropy
before enthalpy gain of crystallization
Notes: The x axis might as well be time, or something like that

## Slide 23: Growth rate: Net crystallisation rate
Net crystallization rate n = Crystallization rate less melting rate
    Crystallization rate: Stems join ncr
    Melting rate: Stems leave lamellae nmelt
    (assuming DG/kBT << 1)
     Net growth rate (ncr – nmelt) =
    t-1: microscopic ‘trial’ frequency ~ h-1, a = size of repeat unit
    DS(L), DG(L) = ? Then find max. n(L)

## Slide 24: Entropy / Enthalpy of crystallizing chain
  DS proportional to number of crystallizing repeat units, Nstem = L/a: DS/kB = mL/a = DS(L)/kB
  DG = 2a2sf - La2DHmDT/Tm(∞) (both per stem)
Enter DG, DS into n- eqn:
Fastest L = L* by dn/dL = 0 
At DT, lamella size L* dominates as it grows faster than all others
P14.1

## Slide 25: Lamella thickness L* vs. DT
Taken from SCM
Good fit to A + B/DT
Lamella, not spherulite, size!
Large lamella  small DT
But slow growth near Tm(∞)
(Polyethylene)
(Data from PJ Barham et al.,
J. Mater. Sci. 20, 1625 (1985))

## Slide 26: Max. growth rate n vs. TC / DT We now know which L = L* grows fastest for given DT But for what DT is n maximum?
 Assume VF scaling for rate, t-1
… difficult to find Tmax analytically,
but expression is dominated by product of a rising (with T),
and a falling, expt’al. Tmax somewhere above Tg, below Tm(∞)

## Slide 27: Growth rate n vs. TC
n(spherulite) vs. T for a polysiloxane, different Mol. Wt. (N)
Peaks in btwn Tg and Tm(∞)
Btw: Very rough guide, Tg ≈ 0.6Tm(∞)
From RL Young,
‘Introduction to Polymers’

## Slide 28: Summary: Lecture #14 Polymer Crystallisation II
Straightening stems from coil needs activation entropy
- Limits lamella thickness, L: Too thick lamellae grow slowly
Straightened stems joining lamella delivers enthalpy
- Favours larger L: Too thin lamellae grow slowly
At given DT, lamella thickness L* = A + B/DT grows fastest
   L* lamellae dominate, typically L* ≈ (10 … 20) nm
Lamella growth rate n peaks below Tm(∞) / above Tg
- To close to Tm(∞): Slow crystallisation due to small free energy gain
- To close to Tg: High viscosity slows crystallisation
 Limited ‘T window’ for polymer crystallisation, ‘Quenching’
The material contained within this lecture can be found in SCM chapter 8.3